## Slide 1: Innovative Landfill Exploration and Mechanical Processing
J.C. Hernández Parrodi, C. Bobe, C. García López and B. Küppers
Renewi Belgium, UGent, RWTH Aachen and Montanuniversität Leoben
5th International Symposium on Enhanced Landfill Mining Symposium (ELFM V)
February 6th 2020, Leuven - Belgium
The NEW-MINE project has received funding from the European Union's EU Framework Programme for Research and Innovation Horizon 2020 under
Grant Agreement No. 721185; www.new-mine.eu

## Slide 2: Overview
Context
Geophysical exploration of landfill site
Excavation of landfill waste
Mech. (pre-)processing of excavated waste
Sensor-based sorting
Conclusions
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium

## Slide 3: Context
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium
Consortium of 17 partners
Test and study implementation of ELFM
  Legacy landfills & dumpsites
  Environmental & health impacts
  Land reclamation
  Waste-to-material (WtM)
  Waste-to-energy (WtE)
Universities, research institutions and industry
EU research program

## Slide 4: Context
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium

## Slide 5: Context
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium
MSG landfill
NEW-MINE´s case study on implementation of ELFM
Excavation zone
Excavated volume
Landfill site in Mont-Saint-Guibert (MSG), Belgium
Old part of landfill
  1958 - 2014
MSW, C&D and non-hazardous IW
Geophysical exploration & material excavation in Jul.-Sep. 2017

## Slide 6: Geophysical exploration
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium
Exploration of contrasts in electrical properties of waste material
Electrical property = Resistance/Conductance
Contrast in conductance = contrast in material?
1. Estimation of waste volume: Capping thickness estimation

## Slide 7: Induction survey
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium

## Slide 8: Results - Induction survey
North
Conductivity

## Slide 9: Second survey – Waste material
2. Exploration of the electrical conductivity of the waste

## Slide 10: Second survey – Waste material
2. Exploration of the electrical conductivity of the waste

## Slide 11: Second survey – Waste material
2. Exploration of the electrical conductivity of the waste
Large variation in electrical conductivity
= large variation in waste material composition?

## Slide 12: Excavation of LF waste
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium
Waste excavation
Total of ~370 Mg of waste excavated
Avg. bulk density of ~800 kg/m3
Avg. water content of ~30 wt.% (raw state)
Avg. material composition:

## Slide 13: Mech. pre-processing
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium
Ballistic separator Stadler STT 600
Ballistic separation
Landfill waste processed directly after exc.
Avg. throughput ~200 m3/h
  3D fraction
  2D fraction
  Under-screen fraction

## Slide 14: Mech. pre-processing
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium
3 wt.%
4 wt.%
5 wt.%
11 wt.%
77 wt.%
(wt.% in raw state)

## Slide 15: Mech. processing of coarse fractions
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium
 | 3D Fraction |  | 2D Fraction | 
 | 3D > 200 mm | 3D 200-90 mm | 2D > 200 mm | 2D 200-90 mm
RDF | 11,3% | 8,7% | 56,5% | 64,7%
Metals | 5,7% | 5,6% | 1,6% | 2,7%
Inert | 83,1% | 77,5% | 7,1% | 1,3%
Fines <20 mm | *0,0% | 8,2% | 34,8% | 31,2%
   WtE
   WtM

## Slide 16: Mech. processing of fine fractions 90-4.5 mm
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium
Inert fraction
Fe metals
Fine fractions <4,5 mm
WC adjustment
90-30 mm & 30-10 mm
10-4,5 mm
Combustibles fraction
Non-Fe metals

## Slide 17: Mech. processing of fine fractions <4.5 mm
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium

## Slide 18: Mass balance of mech. processing of fine fractions
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium
   RDF
   Substitute for construction aggregates
   Recycling
 Substitute for soil in construction applications
As, Cd, Co, Hg and Pb !
Pb, ammonium-N and hydrocarbon contents !
TOC, Cd, Cu, Hg, Pb, Zn and Ni !

## Slide 19: Sensor-based sorting
Input to SBS:
3D fractions from ballistic sep.:
  200-90 mm
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium
Influences on NIR-detection:
Surface defilements
Humidity alters IR-spectra
Surface roughness
 Impede detection
 Hinders detection
 Improves identification
Influences on ejection:
Input composition influences product yield & purity
Throughput rate = Factor for sorting performance
Heavy fractions from density sep. of fine fractions:
  90-30 mm
  30-10 mm
  10-4.5 mm

## Slide 20: Sensor-based sorting
Potential of SBS in ELFM:
Separation of plastic types (>40 mm)
Sep. of combustible and inert materials
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium
Challenges of SBS in ELFM:
Surface defilements in fine fractions
Legislation inhibiting use of recycling products from ELFM
Economic feasibility
Refuse plastic chips
Inert
Combustible

## Slide 21: Conclusions
Geophysical methods can optimize site exploration
  Correlation between geophysical measurements and waste characteristics still challenging
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium
Potential of landfill-mined waste:
  Waste-to-Material
    Ferrous & non-ferrous metals  Recycled metals
    3D fractions (≥90 mm) and inert material (<90 mm)
     Construction aggregates
    Soil-like fractions (<90 mm)  Soil substitute in construction applications
  Waste-to-Energy
    2D fractions (≥90 mm) and combustible material (<90 mm)  Alternative fuel (RDF)

## Slide 22: Conclusions
5th International Symposium on Enhanced Landfill Mining (ELFM V), February 6th 2020, Leuven - Belgium
In the EU WtM and WtE valorization schemes strongly depend on national and local regulations
Greatest challenge in (E)LFM frequently lays on economic feasibility rather than on technical aspects
Sensor-based sorting can enhance outputs for WtM and WtE schemes
  Can significantly affect economic feasibility

## Slide 23: 5th International Symposium on Enhanced Landfill Mining | February 6th 2020 | Leuven - Belgium
THANK YOU FOR YOUR ATTENTION!
The NEW-MINE project has received funding from the European Union's EU Framework Programme for Research and Innovation Horizon 2020 under Grant Agreement No. 721185;
www.new-mine.eu
Juan Carlos Hernández Parrodi
Renewi Belgium SA/NV
Juan.Carlos.Parrodi@Renewi.com
Christin Bobe
UGent
Christin.Bobe@UGent.be
Cristina García López
RWTH Aachen
Cristina.GarciaLopez@IAR.RWTH-Aachen.de
Bastian Küppers
Montanuniversität Leoben
Bastian.Kueppers@UniLeoben.ac.at